## Slide 1: μSTEM: an introduction to S/TEM simulation using the multislice algorithm
Dr. Hamish G Brown
MONASH SCHOOL OF PHYSICS AND ASTRONOMY

## Slide 2: Talk outline
An introduction to the theorist’s electron microscope
  Microscopy without pesky high vacuum systems, power supplies or sample holders
Why simulate?
  Making sense of white dots
How does multislice work?
  How to:
    Write a multislice code that will fit on the back of an envelope
    Mimic an 11 element quadrupole octopole electron aberration corrector with just two equations
    Make an atom from a table of numbers
Setting up a calculation
  Why:
    Graphics cards are good for more than playing FarCry 5 and Assassins Creed
    Multislice is like Pacman
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 3: The electron microscope: a theorist’s perspective
Conventional transmission electron microscopy (CTEM)
Scanning transmission electron microscopy (STEM)
Plane wave illumination
Sample
Post specimen lens
Image plane
Probe forming lens
Diffraction plane
detector
Sample
≈
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 4: Different scanning transmission electron microscopy (STEM) modes
1. Kothleitner G. et al., “Quantitative elemental mapping at atomic resolution using X-ray spectroscopy”, PRL 112 (2014), 085501
Energy dispersive X-ray (EDX) detector1
Electron energy loss spectroscopy (EELS)1
Annular dark field (ADF)
detector1

## Slide 5: Why simulate TEM images?
Electrons interact strongly with crystalline specimens
Typically no simple relationship between TEM images and structure
Comparing experiment to a simulation for assumed structure is a way around this
2. Hovden, R. et al., "Channeling of a subangstrom electron beam in a crystal mapped to two-dimensional molecular orbitals“, PRB 86 (2012), 195415.
3. Boothroyd C.B. and Stobbs W. M., “The contribution of inelastically scattered electrons to high resolution images of (Al, Ga)As/GaAs heterostructures”, Ultramicroscopy 26 (1988), 361-376
Fig 1: An electron probe converged atop:
Vacuum
A single atomic column
Two adjacent atomic
columns2
Fig 2: The early days of quantitative EM: comparing bright-field TEM simulated defocus thickness montages to experiment3
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 6: Getting more with simulation
With simulation you can:
Count atoms (qHAADF)4
Measure thickness to +/- 1 nm using position averaged converged beam electron diffraction (PACBED)5
Quantify spectroscopic (EDX and EELS) results6
4. LeBeau et al., “Standardless atom counting in scanning transmission electron microscopy”, Nano Letters 10 (2010), 4405-4408
5. LeBeau et al., “Position averaged convergent beam electron diffraction: Theory and applications”, Ultramicroscopy 110 (2010), 118-125
6. Chen Z. et al., “Quantitative atomic resolution elemental mapping via absolute-scale energy dispersive X-ray spectroscopy”, Ultramicroscopy 168 (2016), 7-16
Counting atoms with quantitative HAADF4
Quantitative STEM-EDX with thickness measurement by PACBED6
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 7: How do calculations work?
Divide the specimen is into distinct slices
At each slice the multiply probe wave function is by “transmission function” (function of electro-static potential)
Propagate wave between slices with the Fresnel (free space) propagator
1. Multiply wave function by slice transmission function
2. Convolve wave function with Fresnel propagator
Illumination wave function Ψillum
Exit surface wave function Ψexit
Repeat
at each of
N slices
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 8: How do calculations work?
ψillum
ei
ei
FFT
IFFT
ψexit
Transmission function
Propagator
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 9: Actual multislice is only 4 lines of code!
So what are the other 7,000 lines of code for then?

## Slide 10: Making a probe
From Krivanek et al. Ultramicroscopy 78 (1999) 1-11
≈
Aperture function
Aberration function
From Kirkland, Ultramicroscopy 111 (2011) 1523-1530

## Slide 11: Making a sample
Fourier coefficients of electrostatic potential for each atomic species are parametrised in works such that above

## Slide 12
Calculate potential for each atom and shift to unit cell position

## Slide 13: Multislice with Graphical Processor Units (GPUs): not just for play!
GPUs have thousands of cores to process parallel workloads efficiently
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 14: Multislice with Graphical Processor Units (GPUs): not just for play!
The fast Fourier transform (FFT) step is typically the speed-limiting factor in multislice
A GPU will typically perform an FFT 10x faster than a CPU
7. Dwyer C., “Simulation of scanning transmission electron microscope images on desktop computers”, Ultramicroscopy 110 (2010), 195–198
A comparison of CPU and GPU multislice runtimes for a single atomic slice7
Notes: Move equation to next slide. Make this slide less cluttered.

## Slide 15: Running a calculation
Notes: Make red box

## Slide 16: Setting up a calculation: the xtl file
Unit cell dimensions and internal angles
Accelerating voltage (kV)
Number of different elements
Atomic number (Z)
Fractional occupancy
Mean-squared thermal displacement (Debye-Waller factor)
Atomic coordinates (fraction of the unit cell)
Number of atoms
Sr
O
Ti-O

## Slide 17: Setting up a calculation: unit cell sub-slicing
The multi-slice assumptions are only correct in the limit that the thickness of the slices are small
We often sub-slice the unit cell
Aim for slices around 2 Å

## Slide 18: Setting up a calculation: unit cell tiling
Like classic arcade game Pacman, a Multislice calculation uses periodic boundary conditions
In STEM, to stop our probe expanding past the edge of our grid we do calculations on a “supercell” (a tiling of the crystal)
If

## Slide 19: Setting up a calculation: grid sampling
Choose a pixel grid size that gives a fine enough sampling of the atoms (~ 10 pixels per Angstrom)
One way that we can check this is to monitor if electrons are lost to the calculation (the “Intensity” value is significantly less than 1) – more on this later
1024x1024 pixels
256x256 pixels
128x128 pixel calculation ☹️
1024x1024 pixel calculation 😊
60-200 mrad
HAADF detector

## Slide 20: Thermal scattering model
Quantum Excitation of Phonons (QEP) model
  accurately calculates both the elastic and inelastic scattering6
Absorptive model
  Accurately calculates elastic scattering and approximates thermal scattering
The absorptive model takes an order of magnitude less time to compute
6. Forbes B.D. et al., “Quantum mechanical model for phonon excitation in electron diffraction and imaging using a Born-Oppenheimer approximation”, PRB 82 (2010), 104103
(a) Elastic and inelastic components (log scale) and (b) just elastic components
of the diffraction pattern from CBED of a 60 A thick SrTiO3 sample6

## Slide 21: So how bad is the absorptive model exactly?
For samples thicker than 20 nm the absorptive model doesn’t accurately calculate STEM HAADF images
Same with STEM EDX and EELS simulations: inelastically scattered electrons ionize atoms too and ignoring this leads to incorrect results7
Use absorptive for quick, exploratory calculations and QEP for the publication
Sr column
Ti/O column
In between columns
Calculated and experimental HAADF intensities7
Fraction of probe inelastically scattered in SrTiO38
7. LeBeau J. M.. et al., “Quantitative atomic resolution scanning transmission electron microscopy”, PRL 100 (2008), 206101
8. Forbes B.D. et al., “Contribution of thermally scattered electrons to atomic resolution elemental maps”, PRB 86 (2012), 024108
Notes: Correct citation for PRL frozen phonon vs BW paper

## Slide 22: Setting up a QEP calculation
Because I used an 8x8 tiling I effectively get a factor of 8x8=64 times more transmission functions!! 😊😊😊

## Slide 23: Setting up a QEP calculation
The number of passes for STEM imaging is usually 25-40 but can be up to 1000 if we want to see accurate Kikuchi bands in diffraction! There are no hard rules, keep increasing the number until the image stops changing.
Notes: Slow down GIF

## Slide 24: Setting up a QEP calculation
This determines the seed for the random number generator, if kept the same it ensures reproducibility of calculations

## Slide 25: Go forth and simulate! (but have lunch first)
Al3Li STEM
Si3N4 TEM\ Diffraction
Si110 PACBED
SrTiO3 STEM EDX
Or choose your own adventure…

## Slide 26: Acknowledgements
Hamish Brown is the current maintainer of the μSTEM code.
Les Allen, Adrian D'Alfonso and Scott Findlay originally took the initiative to make this code publicly available, with Adrian D'Alfonso taking on the considerable task of setting up the GPU code. Hamish Brown and Ben Forbes have subsequently made substantial refinements and extensions, with Ben Forbes responsible for several efficiency improvements. The code was developed mainly at the University of Melbourne. We would like to acknowledge the contributions of Mark Oxley and Chris Rossouw to the theoretical and numerical aspects of collaborative research that underpins μSTEM.
In particular, the code IONIZER, whose primary author has been Mark Oxley, was used to set up the parametrized atomic scattering factors for ionization used in μSTEM. Eireann Cosgriff, Torgny Josefsson, Nathan Lugg, Andrew Martin, Gary Ruben and Chris Witte have been members of the group at Melbourne University at various stages and all made contributions to our understanding of inelastic scattering and the simulation thereof.